MIDLANDS LUBRICANTS LTD.

Technical Data Sheet

Mid QUENCH 22

Cold Quenching Oil

Mid quench 22 is a none accelerated quenching oil suitable for at temperatures up to 80°C. It is based on specially selected solvent refined mineral oils to ensure consistent performance under arduous operating conditions. It is formulated to give exceptional thermal stability with maximum resistance to oxidation and sludging.

Mid quench 22 is designed for general purpose applications and is suitable for use in open quench tanks, sealed quench furnaces and continuous furnaces of the shaker hearth, cast link and mesh belt type.

Mid quench 22 is also used where an accelerated quench oi is likely to cause problems such as cracking or distortion when components of high carbon / high alloy steels are being treated.

Applications & Benefits

Sealed or open quench systems up to 80°C

Continuous furnace applications

None accelerated performance

Long life oxidation resistance

Automotive Components

Excellent thermal stability

Arduous conditions and applications

Controls sludge formation and drag out

High flash point

Minimises distortion of components

High Viscosity

| Directions for use |  |  |  |
| --- | --- | --- | --- |
| Shelf life 3 years from date of manufacture |  |  |  |
| Designed to be used as supplied and is safe to use on most metals. |  |  |  |
| Store sealed in a cool dry place between 5°C and 30°C material should always be stored indoors and protected from extremes of temperature. |  |  |  |
| For guidance on handling and disposal please refer to the Material Safety Data Sheet |  |  |  |
| Mid quench 22 |  |  |  |
| Characteristics | Typical Data | Characteristics | Typical Data |
| Appearance | Brown | Specific Gravity | 0.86 |
| Viscosity @ 40°C | 19.6 cst | Flash Point (PMOC) | 200°C |