The Green Alternative to Traditional Antifreeze

Eco Supreme ECO8

Technical Data Sheet

Unlike tradional engine coolants that are based on glycol, a synthetic material derived from fossil fuels, Eco supreme is based on glycerine, a natural material that is a by product from bio-diesel production and is derived from renewable resources.

Midlands Lubricants Eco Supreme is non-toxic to both humans and animals, is non-hazardous to the environment and is readily biodegradable.

Midlands Lubricants Eco Supreme ECO8 is a ready to use product that does not require further dilution for use thereby ensuring the correct concentration is used and problem caused by the use of hard water are eliminated. It employs organic acid technology corrosion inhibitors and is nitrite, amine, phosphate, borate and silicate free.

Physical Properties

|  | Parameter |  |  |  | Method |  |  | EC08 |  |  | ASTM D7714 |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  |  |  |  |  |  | Type II |  |
|  | Appearance |  |  |  | Visual |  |  | Clear liquid * |  |  | Not Specified |  |
|  | Specific Gravity |  |  |  | ASTM D 4052 |  |  | 1.145 |  |  | 1.130 min |  |
|  | 15°C/15°C |  |  |  |  |  |  |  |  |  |  |  |
|  | Equilibrium Reflux |  |  |  | ASTM D 1120 |  |  | 107 |  |  | 106 min |  |
|  | Boiling Point °C |  |  |  |  |  |  |  |  |  |  |  |
|  | Freezing Point °C |  |  |  | ASTM D 1177 |  |  | - 31.5 |  |  | - 27 max |  |
|  | (50% Dilution by vol.) |  |  |  |  |  |  |  |  |  |  |  |
|  | pH |  |  |  | ASTM D 1287 |  |  | 8.5 |  |  | 7.5 – 11.0 |  |
|  | Reserve Alkalinity 0.1N |  |  |  | ASTM D 1121 |  |  | 4 |  |  | Report |  |
|  | HCl |  |  |  |  |  |  |  |  |  |  |  |
|  | Foaming | Vol. (ml) |  |  |  |  |  | 50 |  |  | 150 max |  |
|  | Properties |  |  |  | ASTM D1881 |  |  |  |  |  |  |  |
|  |  | Break (s) |  |  |  |  |  | 1 |  |  | 5 max |  |

* Product can be supplied colourless or dyed in accordance with customer requirements.

Page 1 of 2 pages

TDS/COOLSPEC SUPREME EC08/49355/02 Aug 2017

Corrosion Protection

ASTM D1384 Glassware Corrosion Test Results

|  |  |  |  |  |  |  |  |  | Weight Loss mg/ Coupon |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | Coppe |  |  | Solder |  |  | Brass |  |  |  |  | Steel |  |  | Cast |  |  | Aluminium |  |  |
|  |  |  | r |  |  |  |  |  |  |  |  |  |  |  |  |  | Iron |  |  |  |  |  |
|  | ASTM |  | 10 |  |  | 30 |  |  | 10 |  |  |  |  | 10 |  |  | 10 |  |  | 30 |  |  |
|  | D7714(max) |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  | EC08 |  | 0.6 |  |  | 0.5 |  |  | 1.1 |  |  |  |  | -0.9 |  |  | -1.6 |  |  | -0.6 |  |  |
|  | ASTM D 4340 Corrosion of Aluminium under heat rejecting conditions |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  | Weight Loss mg/ cm²/week |  |  |  |  |  |  |  |  |
|  | ASTM D 3306 (max) |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 1.0 |  |  |  |  |  |  |
|  | COOLSPEC SUPREME EC08 |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 0.3 |  |  |  |  |  |  |

All of the above figures are typical values and do not constitute a specification.

Performance Standards

Midlands Lubricants Eco Supreme ECO8 exceeds the requirements of ASTM D7714 -11 Type II. It also exceeds the requirements for coolants prepared from concentrate meeting BS6580 2010.