MIDLANDS LUBRICANTS LTD.

Technical Data Sheet

5w/40 API SN - Full Synthetic Engine Oil suitable for BMW LL-01 and Renault 0700 - 0710

Product Description

Midlands Lubricants Fully Synthetic 5W/40 is a super multi-grade engine oil produced from high quality synthetic base oils incorporating the latest additive technology to produce a super high performance engine oil that delivers excellent fuel economy. Fully Synthetic 5W/40 has been developed to provide outstanding performance with high fuel economy and is highly recommended and suitable for use in BMW, Porsche and Renault vehicles.

FEATURES / BENEFITS

Excellent Fuel Efficiency and Sludge Control for Stop-Go City Motoring Excellent High and Low Temperature Performance Exceptional Long Term Anti-Wear Characteristics Very High Standard of Engine Cleanliness Long-lasting Dispersant Performance and Corrosion Protection Protects against Ring Sticking at High Temperatures Reduced Oil Consumption and Emissions

PERFORMANCE / SPECIFICATIONS

- API: SN/CF

- ACEA: A3, B4

- MB: 229.3, MB 229.5

- BMW: LL-01

- Porsche A40 VW: 502.00, 505.00

- PAS: B71- 2296

- RN: 0700/0710

- GM: LL-025/A-B

TYPICAL PROPERTIES

- Density, g/cm3 @ 15°C 0.860

- Flash Point, COC 210°C

- Pour Point -35°C

- Viscosity Kinematic, @ 40°C = 75 cSt

- Kinematic, @ 100°C 13.5 cSt

- Viscosity Index 185