MIDLANDS LUBRICANTS LTD.

Technical Data Sheet

10W/40 CK-4 Engine Oil E11

Product Description:

Midlands Lubricants 10W/40 CK4 is a high performance multi-grade low SAPs engine oil incorporating advanced additive technology in superior synthetic base stock. 10W/40 CK4 designed for the very latest Euro VI engines. Suitable for DPF exhaust systems.

Features/Benefits:

Good high and low temperature performance

Good protection against ring sticking at high temperatures, maintaining

oil performance whilst minimising oil consumption and emissions

Very high standard of engine cleanliness

Excellent sludge control protection

Long lasting dispersant, anti-wear and corrosion protection

Performance/Specifications:

10W/40 CK-4 engine oil meets the performance requirements of:

API: CK-4

ACEA: E11, E9-E7

MB: 228.51 Approved

VOLVO – VDS-4.5 Approved

RVI RLD-3 Approved - MACK EOS 4.5 Approved

Ditroit Diesel 93K222 Approved

Voith Class B / MB 235.28

Caterpillar: ECF-3, CNH 3521

MAN M3775 Approved

Sciania Low ash

Cummins CES 20086

JASO DH-2

Typical Properties:

Total Base Number (TBN) 12.5 mgKOH.g-1

Density, g.cm-3 @ 15.5°C 0.877

Flash Point, COC 204°C

Pour Point -40°C

Viscosity

Kinematic, 40°C 87 cSt

Kinematic, 100°C 14.7 cSt

Viscosity Index 177