MIDLANDS LUBRICANTS LTD.

Technical Data Sheet

Super Universal Tractor Oil 10w/30

Product Description

Super Universal Oil 10W/30 SL/CG-4

Midlands Lubricants Super Universal Engine Oil (SUTO) is a high quality/high performance engine oil that meets all the lubrication requirements of farm tractors and agricultural machinery. SUTO is a multi-grade viscosity oil that spans a wide temperature range and is suitable for use in a variety of engines including naturally aspirated and turbocharged diesel and petrol engines. It is suitable for use in tractor hydraulic, transmission, and wet brake systems as well as gear boxes in all farm machinery.

Midlands Lubricants SUTO provides excellent protection under the most arduous operating conditions and is formulated according to the most demanding performance requirements. SUTO includes friction modifier additives to provide smooth operation of the wet brake system to prevent squawk and chatter. SUTO offers the convenience of a single lubricant approach that delivers top performance and avoids the need for stocking of multiple lubricants eliminating the risk of incorrect use in the field.

###### FEATURES/BENEFITS:

Excellent Thermal Stability
Reduced Fuel Consumption
Low Drag Formulation
Reduced Friction
Rapid Circulation on Start-up
Excellent Anti-wear Protection
Reduces Oil Inventory
Lower Emissions
Resists Black Sludge
Improved Engine Cleanliness
Low Oil Consumption
Low Chlorine Formulation (for safe disposal or recycling)

###### PERFORMANCE PROFILE:

API SF/CG-4 – CF-4 
MIL-L-2104C/D, MIL-L-45199B
Caterpillar TO-2 – Allison C4

New Holland: NH 410B, NH 030C
Ford ESN-86A/B,
Ford M2C 159B/C
Ford M2C 134D
John Deere: J27, JD 303, JD 20A, J20C, J14B
Case: MS 1206 – MAT 3525
Massey-Ferguson: M1145 Approved M1139, M1135, M1127A
MIL-L-2105
API GL4
IH B6

TYPICAL PROPERTIES

- TBN 10.3 mgKOH/g

- Density, g.cm-3 @ 15°C 0.881

- Flash Point, COC 223°C

- Pour Point -38°C

- Sulphated Ash 1.17%

- Viscosity Kinematic, 40°C = 62 cSt

- Kinematic, 100°C = 9.7 cSt

- Viscosity Index 141